**Załącznik nr 1 do zaproszenia**

**Specyfikacja techniczna**

1. Przedmiotem jest **dostawa do Narodowego Centrum Badań Jądrowych Ośrodka Radioizotopów POLATOM izotopu wzbogaconego Te-130 w postaci ditlenku telluru Te-130 (TeO2) w ilości 8 kg Telluru (Te)”.**
2. **wymagania techniczne:**

Wymagane wzbogacenie Te-130: ≥ 96,0 %

Pojedyncze chemiczne zanieczyszczenie: ≤ 10 ppm

Sumaryczne chemiczne zanieczyszczenia: ≤ 200 ppm

Opakowanie jednostkowe: 1 - 8 kg

Zamawiający wymaga dostarczenia wraz z dostawą karty charakterystyki produktu oraz certyfikatu jakości.

Zamawiający wymaga realizacji zamówienia w dostawach wg harmonogramu:

**ostatnia dostawa:**

**- w terminie do 15 marca 2023 r.**

**annex No 1 to the invitation**

**Technical Specification**

1. **The subject of the matter is Delivery of 8 kg of Tellurium (Te) enriched isotope Te-130 in the form of tellurium dioxide Te-130 (TeO2) to the National Centre for Nuclear Research POLATOM.**
2. **technical requirements:**

Required enrichment of Te-130: ≥ 96.0 %

Single chemical impurity: ≤ 10 ppm

Total chemical impurities: ≤ 200 ppm

Unit packaging: 1 - 8 kg

The Ordering Party requires a product data sheet and quality certificate to be provided with the delivery

The Ordering Party shall require the execution of the order in deliveries according to the schedule:

**the last delivery:**

**- by March 15, 2023**